Vegamelt Hot Melt - Selic Chemical Company – Thailand
www.selicchemical.com[image: image1.png]




	Product
Name


	Application
	Viscosity

cPs

	Softening
Point
(Ring & Ball)

	Type
	Notes

	Vegamelt
708

	For wood working
	50,000–60,000 cPs @ 149°C

20,000–30,000 cPs @ 177°C

10,000–16,000 cPs @ 191°C

	85-95°C
	Ethylene Vinyl Acetate (EVA) Type
	Application temperature 
140–160°C


	Vegamelt
710

	For wood working
	90,000–110,000 cPs @ 180°C

50,000–70,000 cPs @ 200°C

	115-125°C
	Ethylene Vinyl Acetate (EVA) Type
	Application temperature
190–210°C


	Vegamelt
888

	Premium product for cardboard packaging
	1,200–1,800 cPs @ 160°C
600–900 cPs 
@ 350°C

	100-110°C
	Ethylene Vinyl Acetate (EVA) Type
	Setting Time
4–5 seconds

Open Time

20–22 seconds
Working Temperature
160-180°C


	Vegamelt
9001

	Economy  product for cardboard packaging

	800-1,300 cPs 
@ 160°C
	100-110°C
	Ethylene Vinyl Acetate (EVA) Type
	Setting Time
2-3 seconds

Open Time
12-14 seconds

Working Temperature 160-180°C


	Vegamelt
3000

	For bonding plastic labels to PET bottles. Can be used with PE and PVC bottles also.

	2,500-3,000 cPs @ 160°C
1,500-2,000 cPs @ 180°C

	81.0-87.0°C
	PSA – Pressure Sensitive Adhesive

Styrene-Butadiene block copolymer

	Setting time
2-3 sec

Open time
7-9 sec

Working Temperature

160.0-180.0°C



	Vegamelt
2000

	For book binding

	4,500-5,500 cps at 160°C
2,500-3,500 cps at 180°C

	80-84°C
	EVA Based
	Setting time
3-5 sec

Open time
10-18 sec

Working Temperature

160.0-180.0°C



© Selic Chemical Company Thailand

www.selicchemical.com
Page 2 of 2

[image: image1.png]