Selic Chemical Company – Thailand

www.selicchemical.com
[image: image1.png]




Solvent Based Adhesives for Wood Working, Furniture Manufacturing, Construction
Simple Polychloroprene Grades (also known as Yellow Glue, Synthetic Rubber Glue, CR Glue)

	Product Name


	Notes
	Viscosity

cPs 30°c


	Drying Time 30°c


	Tack Time

30°c
	Appearance

	A-69

	Spray grade for furniture making for Formica, glass, wood, hardboard and sponge bonding

	300 - 350
	15 – 20 minutes
	20 – 30 minutes
	Light 
yellow 
liquid

	A-111

	Long curing time. For Formica, metal, wood and concrete

	6,000 - 6,400
	30 – 40 minutes
	40 – 60 minutes
	Brown
transparent
viscous
liquid

	K-999

	Fast curing time for Formica, metal, glass, wood, plastic and concrete

	8,000 - 8,500
	30 – 40 minutes
	40 – 60 minutes
	Brown
transparent
viscous
liquid

	K-999A

	Long curing time for Formica, metal, glass, wood, plastic and concrete

	8,000 - 8,500
	30 – 40 minutes
	40 – 60 minutes
	Brown
transparent
viscous
liquid

	NIG D-6

	For Formica, glass, wood, fabric, sponge and paper

	4,400 - 4,700
	20 – 30 minutes
	30 – 40 minutes
	Yellow translucent
viscous
liquid

	NL/SR-123


	General purpose
	3,200 - 3,400
	15 – 30 minutes
	20 – 40 minutes
	Yellow translucent
viscous
liquid

	W-999

	Fast curing for  Formica, metal, glass, wood, plastic and concrete

	2,000 - 2,160
	15 – 30 minutes
	20 – 40 minutes
	Light yellow viscous
liquid


	WOLF A-1000


	For Formica, glass, wood, hardboard and sponge
	3,000 - 3,400
	20 – 30 minutes
	30 – 40 minutes
	Light yellow viscous
liquid

	A-420

	For Neoprene rubber, manufacturing of insulation parts and lamination


	3,900 - 4,000
	20 – 30 minutes
	30 – 40 minutes
	Black
viscous
liquid

	A-811

	Toluene free cement for Neoprene, rubber, EVA sponge materials and metal bonding and lamination

	1,200 - 1,400
	15 – 20 minutes
	20 – 30 minutes
	Blue black
viscous
liquid

	A-929


	Long curing time for manufacture of insulation parts
	4,100 - 4,300
	20 – 30 minutes
	30 – 40 minutes
	Dark black
viscous
liquid

	Y-4B

	For bonding Neoprene, rubber, EVA sponge materials to metal


	3,900 - 4,000
	20 – 30 minutes
	30 – 40 minutes
	Blue black
viscous
liquid

	Y-4G

	For bonding Neoprene, rubber, EVA sponge materials to metal


	3,900 - 4,000
	20 – 30 minutes
	30 – 40 minutes
	Dark green viscous
liquid

	Y-444


	For EVA and other foam insulation materials - spray grade


	300 – 400
	15 – 20 minutes
	20 – 30 minutes
	Yellow viscous fluid


	Hi-Bond C-900


	Liquid gasket for sealing components exposed to vibration, shock and certain fuels and oils


	2,600 - 2,800
	20 – 30 minutes
	30 – 40 minutes
	White grey
viscous
liquid

	A-120

	General purpose
	5,500 - 6,000
	20 – 30 minutes
	30 – 40 minutes
	Red
orange
viscous
liquid


	A-120HV

	General purpose
	6,800 - 7,200
	30 – 40 minutes
	40 – 60 minutes
	Red
orange
viscous
liquid


	A-121

	Fast curing
General purpose
	6,300 - 6,700
	30 – 40 minutes
	40 – 60 minutes
	Red
orange
viscous
liquid


	C-88


	General purpose
	5,000 - 5,500
	20 – 30 minutes
	30 – 40 minutes
	Light
yellow
viscous
liquid


	D-8L


	General
purpose
	3,800 - 4,000
	15 – 30 minutes
	20 – 40 minutes
	Yellow
translucent

viscous
liquid


	ES-888
(NRS1061)

	Spray grade for general purpose
	500 - 600
	15 – 30 minutes
	20 – 40 minutes
	Yellow
translucent

viscous
liquid


	S-104


	Spray grade for general purpose


	275 - 325
	15 – 30 minutes
	20 – 30 minutes
	Yellow
translucent
liquid


	S-104A


	Spray grade for general purpose


	275 - 325
	15 – 30 minutes
	20 – 30 minutes
	Yellow
translucent
liquid



	S-114


	Spray grade for general purpose


	275 - 325
	15 – 30 minutes
	20 – 30 minutes
	Yellow
translucent
liquid


	S-222 / S-223


	Spray grade for general purpose
	200 - 250
	15 – 20 minutes
	20 – 30 minutes
	Light
green
liquid



Solvent Based Hardeners

	Selodur RF


	Isocyanate hardener for solvent based Polychloroprene adhesives


	
	35 – 40 minutes
	6.5 – 7.5 minutes
	Light

Yellow

	Selodur RF(E)


	Isocyanate hardener for solvent based Polyurethane and Polychloroprene adhesives


	
	35 – 40 minutes
	3.5 – 3 minutes
	Light

yellow


© Selic Chemical Company Thailand

www.selicchemical.com
Page 1 of 4

[image: image1.png]