www.selicchemical.com

[image: image1.png]



Deltabond Series Water Based Adhesives - Selic Chemical Company – Thailand

	Product
Name


	Application
	Viscosity

mPa.S, 27°C

	Solid
Content

	Type
	Notes

	Deltabond WW209

	For wood working: finger joints and edge gluing
	35,000 – 45,000
#6/10 rpm

	40 +/-1
	PVAc
	Flexible
Suitable for paper cartons
and wood

	Deltabond WW226

	For wood working: laminates
	30,000 – 40,000
#5/10 rpm

	38 +/-1
	PVAc
	1 or 2 parts
Good water resistance

	Deltabond WW238

	For wood working: 

parquet flooring
	30,000 – 40,000
#6/10 rpm

	40 +/-1
	PVAc
	Medium viscosity

	Deltabond WW242

	For wood working: 

parquet flooring and laminates
	14,000 – 17,000
#5/10 rpm

	47 +/-1
	PVAc
	1 or 2 parts
Good weather resistance

	Deltabond PO307

	For packaging and labeling: 
for paper overlay
	35,000 – 45,000
#6/10 rpm

	33 +/-1
	PVAc
	Good resistance to discolouration from mould and blue stain

	Deltabond GP330

	For packaging and labeling: 
for porous materials
	30,000 – 40,000
#6/10 rpm

	22 +/-1
	PVAc
	For paper, carton, wood

	Deltabond 
PT333

	For packaging and labeling: 
for porous materials
	6,000 – 8,000
#5/10 rpm

	40-45 +/-1
	PVAc
	For making paper tubes

	Deltabond 
LB339

	For packaging and labeling: 
for porous materials


	100,000 – 110,000
#7/10 rpm

	20 +/-1
	PVAc
	For labelling glass bottles, paper cartons and textiles


	Deltabond 
LB342

	For packaging and labeling: 
for porous materials


	40,000 – 45,000
#6/10 rpm

	16 +/-1
	PVAc
	For labelling glass bottles, paper cartons and textiles

	Deltabond 
SP421

	For packaging and labeling: 
for PVC and PET bottles


	110,000 – 120,000
#7/10 rpm

	51 +/-1
	EVA
	High wet tack and good adhesion



	Deltabond 
SP446

	For packaging and labeling: 
for PVC and PET bottles


	120,000 – 130,000
#7/10 rpm

	53 +/-1
	EVA
	High wet tack and good adhesion



	Deltabond 
SP401

	For special applications: 
for PVC overlay, gypsum and particle board


	4,000 – 7,000
#4/10 rpm

	50 +/-1
	EVA
	

	Deltabond 
SP402

	For special applications: 
for PVC overlay, gypsum and particle board


	9,000 – 15,000
#4/10 rpm

	50 +/-1
	EVA
	

	Deltabond 
SP407

	For special applications: 
for low energy surface substrate


	16,000 – 18,000
#5/10 rpm

	48 +/-1
	EVA
	Good wet tack



	Deltabond 
SP426

	For special applications: 
for membrane pressing


	2,500 – 4,500
#4/10 rpm


	55 +/-1
	EVA
	Good for foam to cloth and non woven




© Selic Chemical Company Thailand

www.selicchemical.com
Page 1 of 2

[image: image1.png]