Solvent Based Adhesives for Footwear Manufacturing

Simple Polychloroprene Grades (also known as Yellow Glue, Synthetic Rubber Glue, CR Glue)

| Product Name | Notes | Viscosity cPs 30°c | Drying Time 30°c | Tack Time 30°c | Appearance |
| --- | --- | --- | --- | --- | --- |
| A-56 | Good for EVA lamination | 5,000 - 5,500 | 20-30 minutes | 30-40 minutes | Light yellow viscous liquid |
| A-56HV | Good for EVA lamination | 7,500 - 8,000 | 30-40 minutes | 40-60 minutes | Light yellow viscous liquid |
| A-60 | Good for EVA lamination | 5,000 - 5,500 | 20-30 minutes | 30-40 minutes | Red yellow viscous liquid |
| A-88 | Good for EVA lamination | 3,700 - 3,900 | 15-30 minutes | 20-40 minutes | Light yellow viscous liquid |
| A-300 | For leather footwear: unit sole, lasting, insole & heel | 3,000 - 3,400 | 15-30 minutes | 20-40 minutes | Light yellow viscous liquid |
| A-300LV | For leather footwear: unit sole, lasting, insole & heel | 2,500 - 3,000 | 15-30 minutes | 20-40 minutes | Light yellow viscous liquid |
| AP-207LV | For leather footwear: unit sole, lasting, insole & heel | 3,400 - 3,600 | 15-30 minutes | 20-40 minutes | Yellow translucent viscous liquid |
| K-402J | Good for EVA foam, heel, lasting & insole | 2,600 - 2,800 | 15-30 minutes | 20-40 minutes | Yellow translucent viscous liquid |
| KOAT | For leather footwear: unit sole, lasting, insole & heel | 2,000 - 2,160 | 15-30 minutes | 20-40 minutes | Light yellow viscous liquid |
| NRC-2030 | Good for EVA lamination | 3,000 - 3,100 | 15-30 minutes | 20-40 minutes | Light yellow viscous liquid |

| NRS-1061 | Spray grade | 500 - 600 | 15-20 minutes | 20-30 minutes | Yellow translucent viscous liquid |
| --- | --- | --- | --- | --- | --- |
| NRS-3032 | For PU, PVC, EVA, foam materials & lamination | 425 - 475 | 15-20 minutes | 20-30 minutes | Yellow translucent viscous liquid |
| S-751W | For PVC, leather, EVA, unit sole, lasting, insole & heel bonding | 450 - 500 | 15-20 minutes | 20-30 minutes | White translucent viscous liquid |
| S-7555AW | For PVC, leather, EVA, unit sole, lasting, insole & heel bonding | 2,400 - 2,520 | 15-30 minutes | 20-40 minutes | Blue white translucent viscous liquid |
| SB-499 | For PU, PVC, EVA, foam materials & lamination | 200 - 300 | 15-20 minutes | 20-30 minutes | Yellow translucent viscous liquid |
| World Grade | For all materials inc. leather uppers, vulcanised rubber outer sole & Neolite soles | 2,000 - 2,160 | 15-30 minutes | 20-40 minutes | Light yellow viscous liquid |
| Big Yellow | For all materials inc. leather uppers, vulcanised rubber outer sole & Neolite soles | 4,500 - 4,700 | 20-30 minutes | 30-40 minutes | Yellow translucent viscous liquid |

Grafted Polychloroprene Grades

| A-90 | With long tack time. For PVC, PU, leather fashion shoes, sports footwear & sandals | 4,800 - 5,000 | 3 – 4 hours | 3 – 8 hours | Light yellow transparent viscous liquid |
| --- | --- | --- | --- | --- | --- |
| A-90D | For PVC, PU, leather fashion shoes, rubber & EVA foam bonding | 1,900 - 2,100 | 2 – 3 hours | 3 – 5 hours | Light yellow transparent viscous liquid |
| NP-600A | For PVC, PU, leather fashion shoes & shoe heels | 4,400 - 4,600 | 3 – 4 hours | 2 – 3 hours | Light yellow transparent viscous liquid |
| NP-3600 | For PVC, PU, leather fashion shoes, rubber & EVA foam | 3,700 - 3,900 | 3 – 4 hours | 2 – 3 hours | Light yellow transparent viscous liquid |
| NP-3650 | For PVC, PU, leather fashion shoes, rubber & EVA foam | 3,900 - 4,100 | 3 – 4 hours | 2 – 3 hours | Light yellow transparent viscous liquid |
| NP-7020 | For PVC, PU, leather fashion shoes, rubber & EVA foam | 1,900 - 2,100 | 2 – 3 hours | 1 – 2 hours | Light yellow translucent viscous liquid |
| NP-7082 | For PVC, PU, leather fashion shoes, rubber & EVA foam | 2,720 - 2,880 | 2 – 3 hours | 1 – 2 hours | Light yellow transparent viscous liquid |
| NP-7082UV | For PVC, PU, leather fashion shoes, rubber & EVA foam | 2,720 - 2,880 | 2 – 3 hours | 1 – 2 hours | Light yellow fluorescent viscous liquid |
| NP-7093 | For PVC, PU, leather fashion shoes, rubber & EVA foam | 2,720 - 2,880 | 2 – 3 hours | 1 – 2 hours | Light yellow transparent viscous liquid |
| NP-8787 | 3,700 - 3,900 | 3,700 – 3,900 | 3 - 4 hours | 2 – 3 hours | Light yellow transparent viscous liquid |

Polyurethane (PU) Adhesive

| Polynon 150NU | For sports footwear & sandals: fabric, leather, PU, PVC & rubber soles | 2,800 - 3,000 | 2 – 4 hours | 0.5 – 1 hour | Colourless transparent viscous liquid |
| --- | --- | --- | --- | --- | --- |
| Polynon 300NU | Higher viscosity, for sports footwear & sandals: fabric, leather, PU, PVC & rubber soles | 4,500 - 4,800 | 3 – 5 hours | 45 minutes – 1.5 hours | Colourless transparent viscous liquid |
| Polynon 300NUB | Higher viscosity, for sports footwear & sandals: fabric, leather, PU, PVC & rubber soles | 4,500 - 4,800 | 3 – 5 hours | 45 minutes – 1.5 hours | Black viscous liquid |
| Polynon 300NUX | Higher viscosity, for sports footwear & sandals: fabric, leather, PU, PVC & rubber soles | 3,900 - 4,100 | 3 – 5 hours | 30 minutes – 1 hour | Colourless transparent viscous liquid |
| Polynon 330HV | Very high viscosity, for sports footwear & sandals: fabric, leather, PU, PVC & rubber soles | 9,300 - 9,700 | 4 – 5 hours | 45 minutes – 1.5 hours | Colourless high viscosity liquid |
| Polynon 330NU | For fabric, leather, PU, PVC, rubber and neolite | 6,300 - 6,500 | 4 – 5 hours | 45 minutes – 1.5 hours | Colourless high viscosity liquid |

| Polynon 333NU | For fabric-leather, PU, PVC, neolite & rubber | 1,920 – 2,080 | 2 - 4 hours | 30 minutes – 1 hours | Colourless transparent viscous liquid |
| --- | --- | --- | --- | --- | --- |

Modified Toluene Free Polyurethane (PU) Adhesive

| MPU-2000TF | For sports shoes and sandals: fabric, leather, Phylon, PU, PVC & rubber soles | 2,000 - 2,400 | 2 - 3 hours | 30 minutes – 1.5 hours | Colourless transparent viscous liquid |
| --- | --- | --- | --- | --- | --- |
| MPU-3000TF | For sports shoes and sandals: fabric, leather, Phylon, PU, PVC & rubber soles | 3,600 - 4,000 | 2.5 – 3.5 hours | 30 minutes – 1.5 hours | Colourless transparent viscous liquid |
| MPU-5000TF | For sports shoes and sandals: fabric, leather, Phylon, PU, PVC & rubber soles | 5,200 - 5,600 | 3 – 4 hours | 30 minutes – 1.5 hours | Colourless transparent viscous liquid |

Solvent Based Primers For Use With Polychloroprene Adhesives

| P5A/B | Special high strength primer for vulcanized-rubber sole, Neolite sole and TPR sole | 2.0 | 2 – 3 hours | 8 – 10 hours | Colourless transparent liquid |
| --- | --- | --- | --- | --- | --- |
| P-16 | General purpose cleaner for rubber, Neolite and glossy surfaces |  | 2 – 3 hours |  | Light yellow liquid |
| P-82 | Special high strength primer for rubber and Neolite sole | 1.75 - 2.25 | 2 – 3 hours |  | Light yellow liquid |

| P-102 | Special anti yellow primer for EVA mid-sole and EVA foam materials |  | 2 – 3 hours |  | Light yellow liquid |
| --- | --- | --- | --- | --- | --- |
| P-105 | Primer for vulcanized rubber and TPR sole | 9.0 - 9.5 | 2 – 3 hours |  | Light yellow liquid |
| P-910 | Primer for EVA mid-sole and rubber-EVA and neoprene foam materials | 6. 5 - 7.5 | 2 – 3 hours |  | Light yellow transparent liquid |
| P-2400 | Special primer for PVC/PU-leather, PVC/PU sole and Neolite sole, gloss surface | 1.75 - 2.25 | 2 – 3 hours |  | Light yellow liquid |
| S-200 | General purpose primer for PVC/PU-leather, PVC/PU-sole and Neolite sole |  | 2 – 3 hours |  | Light yellow liquid |

Modified Toluene Free Primers For Use With Polyurethane (PU) Adhesives

| MPU-222TF | Primer for leather, PVC and PU materials. Reinforces Phylon and TPU bonding | 15 - 45 | 2 – 3 hours | 4 – 6 hours | Colourless fluorescent liquid |
| --- | --- | --- | --- | --- | --- |
| MPU-323TF | Primer for leather, PVC and PU materials. Reinforces Phylon bonding | 110 - 140 | 2 – 3 hours | 4 – 6 hours | Colourless fluorescent liquid |

| MPU-424TF | For glossy-surface PVC and PU materials | 400 - 500 | 2 – 3 hours | 3 – 4 hours | Colourless fluorescent liquid |
| --- | --- | --- | --- | --- | --- |
| MPU-525TF | For glossy surface PVC and PU materials | 1,000 - 1,200 | 2 – 3 hours | 3 – 4 hours | Colourless fluorescent viscous liquid |
| NU-37TF | For hard EVA sponge, moulded EVA and compressed Phylon materials | 0.55 - 0.75 | 2 – 3 hours |  | Colourless fluorescent liquid |
| NU-39TF | Non-UV primer for soft EVA sponge, moulded EVA and compressed Phylon materials | 3.5 - 4.5 | 2 – 3 hours |  | Colourless fluorescent liquid |
| P-5A/B | For vulcanized and thermoplastic rubber and metal | 2.0 | 2 – 3 hours | 8 – 10 hours | Colourless fluorescent liquid |
| P-6A/B | For vulcanized and thermoplastic rubber and metal | 2.0 | 2 – 3 hours | 8 – 10 hours | Colourless fluorescent liquid |
| P-7A/B | Anti yellow primer for vulcanized and thermoplastic rubber and metal | 1.6 | 2 – 3 hours | 4 – 6 hours | Colourless fluorescent liquid |

Solvent Based Primer To Use With Polyurethane (PU) Adhesives

| P-8A/B | Toluene free anti yellow primer for vulcanized and thermoplastic rubber and metal | 1.6 | 2 – 3 hours | 4 – 6 hours | Colourless fluorescent liquid |
| --- | --- | --- | --- | --- | --- |

| P-105 | For vulcanized rubber and TPR soles | 9.0 - 9.5 | 2 – 3 hours |  | Light yellow liquid |
| --- | --- | --- | --- | --- | --- |
| P-108A | Primer for leather, PVC and PU |  | 2 – 3 hours |  | Colourless transparent liquid |
| P-420 | High-strength primer for leather, PVC and PU materials |  | 2 – 3 hours |  | ??? |
| UV-37TF | Toluene-free UV primer for hard moulded EVA and injected Phylon materials | 2.5 - 3.5 | 2 – 3 hours |  | Colourless fluorescent liquid |
| UV-39TF | Toluene-free UV primer for soft moulded EVA, TPU and injected Phylon materials | 0.2 – 0.6 | 2 – 3 hours |  | Colourless fluorescent liquid |

Solvent Based Hardeners

| Selodur RF | Isocyanate hardener for solvent based Polychloroprene adhesives |  | 35 – 40 minutes | 6.5 – 7.5 minutes | Light yellow |
| --- | --- | --- | --- | --- | --- |
| Selodur RF(E) | Isocyanate hardener for solvent based Polyurethane and Polychloroprene adhesives |  | 35 – 40 minutes | 3.5 – 3 minutes | Light yellow |